TECHNICAL DATA SHEET

ANTI VANDAL PAINT - REF: - 69L001

A thick, sticky, non-drying coating for applying thickly to areas, which may be vandalised.

PACKAGE SIZE					5 Litre

COLOUR						Black

FLASH POINT						Above 32°C

DRYING TIME @ 20°C					N/A

VOLUME SOLIDS					53% (+/- 2%)

RECOMMENDED W.F.T.				200 microns

RECOMMENDED D.F.T.				N/A

THEORETICAL SPREADING RATE			5 Sq. Metres/Litre

THINNERS						No. 2

SHELF LIFE						12 mths

V.O.C.							362 g/litre

SURFACE PREPERATION

Ensure surface is free from rust, moisture, oil or other surface contamination.

APPLICATION

# BRUSH APPLICATION

HEALTH & SAFETY

Refer to M.S.D.S. 69L001 prior to use.

Provide adequate ventilation.  Prolonged skin contact inhalation of vapour must be avoided.  Eye contamination  - Flush with eyewash or warm water for 10 mins.  Clean hands after use.

Any person or company using this product without first making enquiries as to the suitability for the intended purpose does so at their own risk, and Fiesta Industrial Paints Ltd can accept no liability for the performance of the product or for any loss or damage arising out of such use.