TECHNICAL DATA SHEET

Description

A Solvent borne hard wearing Anti Slip single pack Polyurethane Floor Paint for use on cured and or mature concrete, Wood, Metal or Masonry. • Internal use • Provides a non-slip decorative protective coating.

Uses

Suitable for application directly onto clean, dry primed or previously painted concrete. Enhanced durability can be achieved by applying two coats of Polyurethane Floor Paint over concrete Sealer. Possesses good application and flow properties enabling application by brush, roller or spray. Quick and easy to apply

Recommended Application Methods

Conventional or HVLP spray.
Roller.
Brush.

Colour Range

12 Stock Shades

RAL Classic Series

BS 4800 or 381C Range

Brand Match

Drying Time @ 20ºC

Surface dry - 4 hours.
Hard dry 24 hours.
Low temperature/high humidity will impair the drying of the lacquer.
Do not apply when ambient temperature falls below 10ºC or relative humidity exceeds 80%.
Newly coated items should be protected from frost and precipitation.

Dry Film Thickness

5 - 30 u

Wet Film Thickness

15 - 40 u

Theoretical Coverage Rate

8-14m² per litre @ 20μ DFT
coverage rate can be affected by such variables as type and condition of substrate, type of application equipment and individual method of application

Thinners

Use white spirit 
Wash application equipment immediately after use.

Packaging

2.5litre, 5 and 20 litres 
Shelf Life: 2 years from shipment date when stored in unopened, original containers.
Storage: Store in temperature range 5-40ºC

Directions for use

Ensure all surfaces are clean, dry and free from dust, grease, millscale, etc.
Seal container after use.
For further information contact our Technical Service Department

Arcrite Industrial Coatings

Units 4 &5 Major Industrial Estate

Middleton Road

Heysham

LA3 2JZ

arcritepaints.com

HEALTH & SAFETY

For full details see separate Health & Safety Data Sheet.

The information given on this sheet is, to the best of our knowledge, true and accurate. No guarantee of the results implied, or any loss or damage arising out of this material, however, are possible as the conditions of application are beyond our control. This is not withstanding any liability arising from the Consumer Protection Act 1987 and the Health & Safety at Work Act. Health and Safety data is available on this product and should be referred to prior to its use.