TECHNICAL DATA SHEET

POLYURETHANE VARNISH GLOSS - REF: - 53L818

A tough hardwearing, polyurethane Matt finish suitable for use in most industrial and commercial environments.

PACKAGE SIZE					5 Litre, 25 Litre

COLOUR						Clear

FLASH POINT						Above 32°C

DRYING TIME @ 20°C					Surface Dry: 4-6 hours

VOLUME SOLIDS					45% (+/- 5%)

RECOMMENDED W.F.T.				67 microns

RECOMMENDED D.F.T.				30 microns

THEORETICAL SPREADING RATE			14-15 Sq. Metres/Litre

THINNERS						No. 2

SHELF LIFE						12 mths

V.O.C.							420 +/- 20g/litre

SURFACE PREPERATION

Ensure surface is free from rust, moisture, oil or other surface contamination.

APPLICATION

May be applied by brush or roller.  Do not apply too thickly as this may impair through drying.  Where the product is being applied to dusty concrete the first coat should be thinned 3:1 with No 2 Thinners.

HEALTH & SAFETY

Refer to M.S.D.S. prior to use.

Provide adequate ventilation.  Prolonged skin contact inhalation of vapour must be avoided.  Eye contamination  - Flush with eyewash or warm water for 10 mins.  Clean hands after use.

Any person or company using this product without first making enquiries as to the suitability for the intended purpose does so at their own risk, and Fiesta Industrial Paints Ltd can accept no liability for the performance of the product or for any loss or damage arising out of such use.

FIESTA INDUSTRIAL PAINTS LTD

BURNLEY ROAD, HAPTON LANCS BB11 5QR

TEL:01282 775639/FAX:01282 776406