TECHNICAL DATA SHEET

QUICK DRYING HAMMER FINISH - REF: - 53L15

A quick drying hammer finish suitable for use in most industrial environments.  The rapid drying properties of this product enable early handling of painted products and the hammer pattern makes this product particularly suitable for application to castings.

PACKAGE SIZE					5 Litre, 25 Litre

COLOUR						BS 4800, BS 381C, R.A.L.

FLASH POINT						22°C - 32°C

DRYING TIME @ 20°C					Surface Dry: 20 - 40 mins

VOLUME SOLIDS					40% (+/- 2%)

RECOMMENDED W.F.T.				75 microns

RECOMMENDED D.F.T.				30 microns

THEORETICAL SPREADING RATE			12 Sq. Metres/Litre

THINNERS						50/5

SHELF LIFE						12 mths

V.O.C.							516 g/litre

SURFACE PREPERATION

Ensure surface is free from rust, moisture, oil or other surface contamination.

APPLICATION

CONVENTIONAL 	Nozzle Size 50 thou, Atomising Pressure 50 p.s.i., Fluid Pressure 10 p.s.i.

SPRAY

HEALTH & SAFETY

Refer to M.S.D.S. prior to use.

Provide adequate ventilation.  Prolonged skin contact inhalation of vapour must be avoided.  Eye contamination  - Flush with eyewash or warm water for 10 mins.  Clean hands after use.

Any person or company using this product without first making enquiries as to the suitability for the intended purpose does so at their own risk, and Fiesta Industrial Paints Ltd can accept no liability for the performance of the product or for any loss or damage arising out of such use.